Fully Fashion Knitwear

Introduction: based on fabric construction and manufacturing garment.

Knitting: It is a process of fabric manufacture by converting yarn into loop form and then these loops interlock/intermesh/interlooped together which form a structure is called knitting or knitted structure.

Or.

Interlocking of loops which form a structure is called knitting.

Wales: vertical column of knitted fabric.

Course: horizontal column of knitted fabric.

Loop: bending of yarn is called loop.

WPI = Wales per Inch     			CPI = Course per Inch

What is fully Fashion?

Fully fashioning is a method/technique of shaping a knitted structure by increasing or decreasing the number of Wales or needles.

( What are the Advantages & Disadvantages of Fully Fashioning?

Advantage:

- Production is effective (Less manpower in design or pattern sector)

- Zero wastage

- Sealed edge garment or quality edge garment.

Disadvantage:

Low volume of production (For needle increasing or decreasing)

( Textiles: Anything that can be originated/generated from fiber.

( Clothing: Ready to wear

( Fiber: Fibers are natural or chemical structure that can be spun into yarn.

( Classic Functions of Textile fiber: Based on sourcing-

( Circular knitting: Needles are arranged in circular way that why is called circular knitting. Two types of needle bed are used in circular knitting machine.

- Dial needle bed &

- Cylinder needle bed

( Fabric: Fabric is an assembly of fiber or yarn which form a structure and which has length, width and thickness.

( Dia: Maximum distance inside the circular is called dia.

( Gauge: Gauge indicates the thickness.

( Flatbed: Needle are arrange in flat way is called flatbed or V-bed.

Fibers Properties

- Mechanical Process: This is the response to applied forces and recovery like-

  - Abrasion resistance

  - Flexibility

  - Stress

- Absorption properties: This is a measure of the quantity of water vapor or liquid water or absorbed by fabric.

  - Water vapor absorption

  - Water absorption

- Thermal properties: The behavior of textile in the presence of heat or when exposed to a flame.

  - Heat resistance capacity or

  - Specific heat

Fibers Identification

| Test | Wool | Acrylic | Cotton |
| --- | --- | --- | --- |
| Burning test/ Flammable test | Non-flammable, Hair burn smell | Flammable Petroleum flame | Flammable Paper burn smell |
| Microscopic test (Cell structure of yarn) |  |  |  |
| Chemical test (acid & alkalis) wet finish | Acid (+) Alkalis (-) | Acid (+) Alkalis (+) | Acid (-) Alkalis (+) |

Based on fibers length:

Textile Yarn: Twisted form of fibers is called yarn.

According to ASTM (American Society for Testing & Material) A generic term for a continuous stand of textile fibers is called yarn.

Classification of Textile yarn:

Spun yarn: Spun yarn are made by twisting together of fibers.

Filament yarn: Filament yarns are made by the assembly of continuous filament.

Mono-filament: Consists of only a single continuous.

Multi filament: Made from multiple filaments.

Complex/Novelty/Fancy: This has special effects on its own appearance.

Cords: cords are made by twisted plied yarn.

Cables: Cables are produced by plying cords.

Slub yarns: Contains partially bulky/fluffy region.

Loop yarns: This yarn requires a base yarn (core yarn) around which the fancy or effect yarn is wrapped.

Common yarn used in the fully fashioned knitwear like-

Basic type:

  - 100% Acrylic

  - Acrylic mélange

  - Blended Acrylic

  - 100% wool

  - Mixed wool

  - 100% cotton

  - Blended cotton

Fancy type:

  - Chenille

  - Angora tweed

  - Nep/slub yarn

  - Loop yarn (Popcorn, Boucle)

  - Mohair

  - Tape yarn

  - Kashmere like etc.

SMM = Spinning Metric Measurement

DMM = Dyeing Metric Measurement

Properties of Yarn

Wool:

  - Bulky/fluffy appearance

  - Poor strength

  - Good resistance to acid

  - Poor resistance to sun-light and insects

  - End use for sweater and suiting

  - Mainly fibers collects from sheep fleece

  - Garment become heavier and also more weighted

  - Garment appearance is not shine

  - More expensive product

  - Warmth feelings

Acrylic:

  - Sources are Acrylonitrille – Ethylene or Acetylene

  - Bulky/fluffy appearance like wool

  - More shiny than wool

  - Good strength

  - Light in weight

  - Good resistance to sun-light and insects

  - Wet finish & dry finish applied

  - End uses heavy knitwear product

  - Less expensive than wool

  - Warmth feeling

Cotton yarn:

  - Smooth surface

  - Cool feeling (suitable for hot)

  - More expensive

  - Moisture absorbency high

Chenille Yarn:

> Source – Cotton chenille			Acrylic chenille

Types of Chenille:

  - Lurex

  - Rayon

  - Rainbow

  - Feather

  - Space dyed

Characteristics of Chenille:

  - Non-washable

  - Non-twistable

  - Velvety appearance

  - Suitable for ladies & babies wear

Kashmery yarn:

  - Non-washable

  - Silky appearance

  - Collected from Kashmeri goats

  - Light strength

Production sequence of fully fashion knitwear (Sweater):

Activities for yarn receive:

Receive yarn by package

. Hank form – Cotton yarn

. Cone form – Accept cotton yarn

Warehouse activities

. Random inspection

. Weight

. Lab dips color match

Winding Section:

. Covert yarn from hank to cone

. For easy knitting

. Number of cone depends of ply

Wastage % of yarn depends on some factors:

- For normal gauge except Chenile yarn wastage % = 4%

- For fine gauge except Chenile yarn wastage % = 5%

Different types of stitches & designs used in Fully Fashion knitwear:

| Basic Category: | Fancy Category: |
| --- | --- |
| Single Jersey Rib category stitch Double Jersey | Shaker or Half Cardigan stitch Full Cardigan stitch Drop knit Tuck Stitch Milano Stitch Poinal Stitch Zigzag Stitch Cables (Different types) Diamond (Different types) |

Single Jersey

Common Name: Jersey stitch, Single Knit, Basic Type Stitch, Plain Knit etc.

Priorities of Single Jersey:

- Appearance: Different appearance in alternate side.

  - Technical Front – Look like V-shape stitch/jersey stitch

  - Technical Back – look like Semi-circle stitch/purl stitch

Stitch diagram of Single Jersey:

| T/B | ( ) | ( ) | ( ) | ( ) |
| --- | --- | --- | --- | --- |
| T/F | V | V | V | V |

| Loop diagram of Single jersey: |
| --- |
| Technical Face: | Technical Back: |

- Edge Curling: Curling produce for yarn tension/torque.

To reduce edge curling-

  - For Heavy knitting – After knitting before linking use Iron at the edge.

  - For light knit – After knitting before sewing use Iron at the edge.

- Dimensional Stability: Dimensional stability is poor of single jersey.

To increase dimensional stability:

  - Increase Loop density

  - Apply resin finish

- Unraveled: We can unravel the yarn from the both end.

- Elasticity: Good elasticity in width wise direction.

- Laddering: Laddering can be repaired in flat bed knitting but not in circular knitting.

Cause of laddering:

> Needle Head Broken

> Poor Quality materials

> Lose tension

- Density: The density of single jersey is light.

- End uses: All basic sweaters, cardigans, pullovers for heavy knit.

Basic T-shirt, polo shirt for light knit.

9. Diagram & Notation:

| Needle Diagram | Stitch Diagram | Notation |
| --- | --- | --- |
|  | T/B ( ) ( ) ( ) ( ) T/F V V V V | T/B O O O O T/F × × × × |

Rib Knitted Structure

The word ‘rib’ derives from animal ribs. In this structure needles head are no t facing directly each other. Rib fabrics are composed of loops formed in opposite direction. Various types rib construction are there but common structure are 1×1 & 2×2 and above 2×2 construction like 3×3, 4×4, 5×5 are Fancy rib but 6×6 rib has special name like Derby rib.

Priorities of Rib:

- Appearance: Both sides should be same in appearance but semi circle loops observe in between ‘V’ shape loops.

Stitch diagram of Single Jersey:

| T/B | ( ) | V | ( ) | V |
| --- | --- | --- | --- | --- |
| T/F | V | ( ) | V | ( ) |

Loop diagram of 1(1 Rib:

- Edge curling: This fabric does not curl at the edges. It is a balance fabric because of having Wales in both directions. The reason is both T/F and T/B bed are active, so tension is uniform on both sides.

- Dimensional stability: Dimensional stability is good.

- Unraveled: We can unrope the structure from the end section only (because it forms from double bed).

- Elasticity: Elasticity can be observed well in widthwise direction.

- Laddering: Laddering can be repaired in flat bed knitting but not in circular knitting.

- Density: Density is heavier than single jersey because loops catch at both sides.

End Uses:

  - Bottoms, collar, cuff, hem and for also for full dress.

  - Especially lightweight for undergarments because elasticity is good.

9. Diagram & Notation:

| Needle Diagram | Stitch Diagram | Notation |
| --- | --- | --- |
|  | T/B ( ) V ( ) V T/F V ( ) V ( ) | T/B ( ( ( ( T/F ( ( ( ( |

Double Jersey

If the plain stitches are one behind the other the fabric/ structure is known double jersey.

Needle diagram of Double Jersey:

Properties/Identification:

    - Appearance: Both sides are same in appearance. Both technical front and technical back has V shape stitch/ jersey stitch.

Stitch diagram of Double Jersey:

| T/B | V | V | V | V |
| --- | --- | --- | --- | --- |
| T/F | V | V | V | V |

Loop diagram of Double jersey:

    - Edge curling: This fabric also does not curl at the edges. Reason is that it is more balanced fabric because all needles are active on both sides (T/F and T/B bed). So tension is uniform on both sides.

    - Dimensional stability: Dimensional stability is very good.

    - Unraveled: We can unrope the structure from the end section only (because it forms from double bed).

    - Elasticity: In comparison to other knit fabric; (especially rib) elasticity is poor.

- Laddering: Laddering can not be repaired in both flat bed knitting and circular knitting. Because both side needles are active at opposite direction.

- Density: In comparison to other knit fabric; density is heavier.

End Uses:

- Normally for heavy knitwear Vast because it is fitted.

- Light knitted is preferred for sportswear (sports T-shirt) because it absorbs sweat well and dimensional stability is good.

- For ladies skirt. And also for tube fabric to make pocket.

9. Diagram & Notation:

| Needle Diagram | Stitch Diagram | Notation |
| --- | --- | --- |
|  | T/B V V V V T/F V V V V | T/B ( ( ( ( T/F ( ( ( ( |

Differences between Single jersey and Rib knit:

| Key Words | Single Jersey | Rib Knit |
| --- | --- | --- |
| 1. Appearance | T/F has V shape stitch and T/B has semi circle stitch. | Semicircle loops can be observed in between V shape loops at both sides. |
| 2. Edge curling | Edge curling occurs. | Edge curling does not occur. |
| 3. Dimensional Stability | Dimensional stability is comparatively poor. | Dimensional stability is good. |
| 4. Unraveled | Can be unroped the yarn from the both end. | Can be unroped the yarn from only the end section. |
| 5. Elasticity | Almost equal elasticity both in lengthwise and widthwise direction. | Elasticity can be observed well in widthwise direction. |
| 6. Needle Bed | Manufacturing by using only T/F needle bed. | Manufacturing by using both T/F and T/B needle bed. |
| 7. Density | Density is lighter than Rib knit. | Density is heavier than single jersey |
| 8. End uses | All basic sweaters, cardigans, pullovers for heavy knit. Basic T-shirt, polo shirt for light knit. | Bottoms, collar, cuff, hem and for also for full dress. Especially lightweight for undergarments because elasticity is good. |
| 9. Fabric Notation | T/B ( ( ( ( T/F ( ( ( ( | T/B ( ( ( ( T/F ( ( ( ( |
| 10. Needle Set | Made by one set of needle; i.e. cylinder needle. (In case of circular knitting) | Made by two set of needle; i.e. dial needle and cylinder needle. (In case of circular knitting) |

Similarities between Single jersey and Rib knit:

- Both is mandible (Laddering can be repaired)

Differences between Single jersey and Double Jersey:

| Key Words | Single Jersey | Double Jersey |
| --- | --- | --- |
| 1. Appearance | T/F has V shape stitch and T/B has semi circle stitch. | Both T/F and T/B has V shape stitch. |
| 2. Edge curling | Edge curling occurs. | Edge curling does not occur. |
| 3. Dimensional Stability | Dimensional stability is poor. | Dimensional stability is very good. |
| 4. Unraveled | Can be unroped the yarn from the both end. | Can be unroped the yarn from the end section only. |
| 5. Elasticity | Elasticity is better than double jersey.direction. | Elasticity is poor. |
| 6. Needle Bed | Manufacturing by using only T/F needle bed. | Manufacturing by using both T/F and T/B needle bed. |
| 7. Density | Density is lighter than double jersey. | Density is heavier than single jersey. |
| 8. Laddering | It is mandible (Laddering can be repaired) | It is not mendable (Laddering can’t be repaired |
| 9. Hand Feel | It is comparatively soft | It is comparatively hard. |
| 9. End uses | All basic sweaters, cardigans, pullovers for heavy knit. Basic T-shirt, polo shirt for light knit. | > Normally for heavy knitwear Vast because it is fitted. > Light knitted is preferred for sportswear (sports T-shirt) because it absorbs sweat well and dimensional stability is good. > For ladies skirt. And also for tube fabric to make pocket. |
| 10. Fabric Notation | T/B ( ( ( ( T/F ( ( ( ( | T/B ( ( ( ( T/F ( ( ( ( |
| 11. Needle Set | Made by one set of needle; i.e. cylinder needle. (In case of circular knitting) | Made by two set of needle; i.e. dial needle and cylinder needle. (In case of circular knitting) |

Note: No similarities between Single Jersey & Double Jersey.

Differences between Rib and Double Jersey:

| Key Words | Rib | Double Jersey |
| --- | --- | --- |
| 1. Appearance | Have semi-circle loops in between V shape stitches at both sides. | Do not have semicircle loops; only V shape stitches at both sides. |
| 2. Elasticity | Elasticity is good. | Elasticity is poor. |
| 3. Density | Density is lighter than double jersey. | Density is heavier than Rib. |
| 4. Dimensional Stability | Dimensional stability is good. | Dimensional stability is better than rib. |
| 5. Laddering | It is mendable (Laddering can be repaired) | It is not mendable (Laddering can’t be repaired) |
| 6. Needle active | All needles are not active of both beds. | All needles are active of both beds. |
| 7. End uses | Bottoms, collar, cuff, hem and for also for full dress. Especially lightweight for undergarments because elasticity is good. | > Normally for heavy knitwear Vast because it is fitted. > Light knitted is preferred for sportswear (sports T-shirt) because it absorbs sweat well and dimensional stability is good. > For ladies skirt. And also for tube fabric to make pocket. |
| 8. Fabric Notation | T/B ( ( ( ( T/F ( ( ( ( | T/B ( ( ( ( T/F ( ( ( ( |

Similarities between Rib and Double Jersey:

- Both side same in appearance.

- Can be unroped the yarn from only the end section.

- Edge curling does not occur.

- Both are double bedded structure. Manufacturing by using both T/F and T/B needle bed.

- Made by two set of needle; i.e. dial needle and cylinder needle.

Process Breakdown of Fully Fashioned Knitwear

Body Panel (Front or Back):

Needle select for bottom rib by needle selector; i.e. 1×1 rib or 2×2 rib

Prepare rib height (as per requirement) By giving courses

Loop transfer from back needle bed to front needle bed (if the body panel is in jersey) By transfer comb

Knit upto armhole starts point

Create armhole (depends on styling) By decreasing or increasing, decreasing both.

Sleeve Panel:

Needle select for cuff rib by needle selector; i.e. 1×1 rib or 2×2 rib

Prepare rib height (as per requirement) By giving courses

Loop transfer from back needle bed to front needle bed (if the sleeve panel is in jersey) By transfer comb

Knit upto armhole line starts point

Linking:

Linking right shoulder

Attach collar rib

Link left shoulder

Attach sleeve panel

Side seam close

End of operation

# Text boxes

Apparel sector

Woven

Knitwear

Cut and Sew

- T-Shirt

- Polo Shirt

Fully Fashion

- Sweater

- Cardigan

- Pullover

Loop

Yarn

Wales

Course

Knitted Structure

Weft knitted structure

Flatbed knitting

Circular knitting

Warp knitted structure

Knitted Structure

Small dia M/C

Circular knitting

Fabric for clothing like:

> Rib knitted structure

> Double Jersey/interlock

>Lactose or Pique

T-shirt, Polo-shirt, Briefs.

Hand Driven

> Driven manually

> Can produce limited design

>Low volume production

> Integrated garment not possible

Power Driven

> Driven by power

> Unlimited design

> High volume production

> Integrated garment possible

Socks

Sweater, Pullover, Cardigan

Tricot

Rachel

Sleeve panel by increasing

Decrease (-)

End product

Mostly non-apparel items

>Mosquito net

> Mesh fabric

> Power net

> Fish net

> Laces etc.

Body

panel

Increase (+)

Decrease (-)

Spinning process/ Giving twisted

Body

panel

Yarn

Textile fiber

Natural

Chemical/man-made

Animal

Plant/Vegetable

Cotton

Wool

Acrylic

Dial needle bed (Horizontal way)

Cylinder needle bed (Vertical way)

Technical Back

Technical front

1. Hand driven

2. Power Driven

Acrylic & others

Cotton

Wool

Long staple

Short staple

Filament

Staple

Fiber

(1.27cm - 6.34 cm)

(3.8cm - 38cm)

(0-2000meter or more)

Mono

Cables

Plied

Multi

Single

Cords

Complex/

Novelty/

Fancy

Simple

Filament yarn

Spun yarn

Textile yarn

Twisted

Flat

1. Mono filament:

2. Multi filament:

3. Staple:

4. Two ply yarn:

5. Multi ply:

6. Cords:

7. Cable:

8. Loop yarn:

Hard & less velvety

Soft & more velvety

Yarn cone distribution section

Winding section

Knitting section

Store / Warehouse

Yarn (Receive from textile)

Washing section

Mending section

Linking continue/Trimming section

Linking section

Button hole

Finishing section

Pressing & ironing

Drying section

Yarn inspection by random process

Knitting inspection

Linking inspection

Light check inspection

Labeling like-

Main label

Size label

Care label

Folding

Ready for export

Final pack

Quality audit by internal expert/quality circle team

Button attach

(If required)

Price tag/

Hang tag

Primary

packaging

Secondary/

Packagin

Final inspection by buyer’s representative using AQL chart

3G	5G 	7G

Normal/Regular gauge

10G	 	12G

Fine gauge

Merchandising

Production

Wastage

Needle Diagram

Technical front

Technical Back

Pull

Pull

Technical front

Needle Diagram: 1×1 rib

Technical Back

T/B

T/F